Cu vs. SWCNT Bundle Interconnect: Detailed Comparative Analysis

RLC Parameters, Circuit Simulation, and Technology Scaling (45 nm → 7 nm)

NOTE All RLC values are extracted directly from CNT_Cu_RLC_Calculations_corrected.xlsx (Summary sheet, data_only mode). Circuit simulation results are read from interconnect.pdf (18 pages of LTSpice transient waveforms). Technology nodes covered: 45 nm, 14 nm, 7 nm at lengths 100 μm, 500 μm, 1000 μm.

# 1. Physical Models & Formula Summary

## 1.1 Copper (Cu) Interconnect

| Parameter | Formula | Description |
| --- | --- | --- |
| Resistivity | ρ_eff = ρ_FS × ρ_MS × ρ₀ | Combines surface + grain-boundary scattering |
| ρ_FS (Fuchs-Sondheimer) | ρ_FS/ρ₀ = function of p (specularity), λ/D | Surface scattering at wire sidewalls |
| ρ_MS (Mayadas-Shatzkes) | ρ_MS/ρ₀ = 1 + (3/2)α − 3α² + 3α³ ln(1+1/α) | Grain-boundary scattering, α = (λ/D)·R/(1−R) |
| Capacitance | Sakurai-Tamaru formula (ITRS-fitted) | Accounts for fringe fields and neighboring wires |
| Self-Inductance | Neumann rectangular-wire formula | L = (μ₀/2π)[ln(2l/(W+H)) + 0.5 + 0.2235(W+H)/l] |

## 1.2 SWCNT Bundle Interconnect

| Parameter | Formula | Description |
| --- | --- | --- |
| Quantum Resistance | R_Q = h/(4e²) ≈ 6,453 Ω | Per CNT, 4 conducting channels |
| Scattering Length | λ_eff = 1/(1/λ_AC + 1/λ_OP) = 49.1 nm | AC phonon: 400 nm at 300 K; OP phonon: 56 nm |
| Bundle Resistance | R = (R_Q + R_Q·L/λ_eff + R_contact)/N_m | Contact resistance included |
| Kinetic Inductance | L_K = h/(4e²·v_F) per CNT | Dominant inductance at short lengths |
| Magnetic Inductance | L_M = (μ₀/2π)·ln(2H/W+1) | Conventional magnetic flux contribution |
| Quantum Capacitance | C_Q = 4e²/(h·v_F) per CNT | Quantum electrostatic effect |
| Electrostatic Cap. | C_E = 2πε₀ε_r/ln(2y/d_bundle) | Geometric capacitance |

# 2. Technology Node Parameters

| Node | W (nm) | H (nm) | W_eff Cu (nm) | H_eff Cu (nm) | N_total CNTs | N_metallic CNTs |
| --- | --- | --- | --- | --- | --- | --- |
| 45nm | 45 | 90 | 38 | 73 | 897 | 299 |
| 22nm | 22 | 45 | 18 | 37.6 | 350 | 117 |
| 14nm | 14 | 28 | 11 | 25.1 | 190 | 63 |
| 7nm | 7 | 14 | 5 | 13 | 72 | 24 |

IMPORTANT The effective Cu cross-section (W_eff, H_eff) shrinks due to barrier metal thickness. At 7 nm, only 5 nm width remains for current flow, dramatically amplifying scattering effects. CNT bundle size also decreases, reducing N_m from 299 to 24 metallic SWCNTs.

# 3. Copper Effective Resistivity Scaling

| Technology Node | ρ_FS Multiplier | ρ_MS Multiplier | ρ_eff (μΩ·cm) | vs. Bulk Cu (1.68 μΩ·cm) |
| --- | --- | --- | --- | --- |
| 45 nm | 1.163 | 1.247 | 2.43 | 1.45× |
| 22 nm | 1.332 | 1.495 | 3.35 | 2.00× |
| 14 nm | 2.601 | 1.769 | 7.73 | 4.60× |
| 7 nm | 3.984 | 2.514 | 16.83 | 10.02× |

Key Insight: Copper resistivity degrades 10× above bulk at 7 nm. The escalation is non-linear — it roughly doubles again between 14 nm and 7 nm, driven by simultaneous intensification of both surface scattering (ρ_FS multiplier nearly 4×) and grain-boundary scattering (ρ_MS multiplier 2.5×).

# 4. Complete RLC Data Tables

## 4.1 Resistance Comparison (Ohm)

### Length = 100 μm

| Node | Cu R (Ω) | CNT R (Ω) | CNT/Cu Ratio |
| --- | --- | --- | --- |
| 45 nm | 877.7 | 43,991 | 50.1× |
| 22 nm | 4,946 | 112,422 | 22.7× |
| 14 nm | 28,006 | 208,783 | 7.5× |
| 7 nm | 258,858 | 548,055 | 2.1× |

### Length = 500 μm

| Node | Cu R (Ω) | CNT R (Ω) | CNT/Cu Ratio |
| --- | --- | --- | --- |
| 45 nm | 4,389 | 219,735 | 50.1× |
| 22 nm | 24,730 | 561,546 | 22.7× |
| 14 nm | 140,028 | 1,042,870 | 7.4× |
| 7 nm | 1,294,291 | 2,737,535 | 2.1× |

### Length = 1000 μm

| Node | Cu R (Ω) | CNT R (Ω) | CNT/Cu Ratio |
| --- | --- | --- | --- |
| 45 nm | 8,777 | 439,415 | 50.1× |
| 22 nm | 49,461 | 1,122,950 | 22.7× |
| 14 nm | 280,057 | 2,085,479 | 7.5× |
| 7 nm | 2,588,583 | 5,474,384 | 2.1× |

WARNING CNT resistance is dominated by quantum and contact resistance (R_Q = 6,453 Ω per CNT). At 100 μm, the scattering contribution is small relative to R_Q, so the CNT/Cu ratio holds ~constant across lengths. At 7 nm, Cu approaches CNT resistance (only 2.1× apart), signaling the crossover regime.

## 4.2 Inductance Comparison (nH)

### Length = 100 μm

| Node | Cu L (nH) | CNT L (nH) | CNT/Cu Ratio |
| --- | --- | --- | --- |
| 45 nm | 0.158 | 2.727 | 17.2× |
| 22 nm | 0.172 | 6.925 | 40.3× |
| 14 nm | 0.180 | 12.835 | 71.3× |
| 7 nm | 0.193 | 33.643 | 174.3× |

### Length = 500 μm

| Node | Cu L (nH) | CNT L (nH) | CNT/Cu Ratio |
| --- | --- | --- | --- |
| 45 nm | 0.952 | 13.637 | 14.3× |
| 22 nm | 1.019 | 34.625 | 34.0× |
| 14 nm | 1.061 | 64.177 | 60.5× |
| 7 nm | 1.127 | 168.213 | 149.3× |

### Length = 1000 μm

| Node | Cu L (nH) | CNT L (nH) | CNT/Cu Ratio |
| --- | --- | --- | --- |
| 45 nm | 2.042 | 27.275 | 13.4× |
| 22 nm | 2.178 | 69.250 | 31.8× |
| 14 nm | 2.261 | 128.353 | 56.8× |
| 7 nm | 2.393 | 336.426 | 140.6× |

NOTE CNT inductance is dominated by kinetic inductance (L_K). For the 7 nm bundle with only 24 metallic SWCNTs, L_K_bundle = 336 pH/μm vs magnetic inductance of only 0.32 pH/μm — a 1000× difference. Cu's conventional magnetic inductance is relatively flat with node scaling (0.16–0.19 nH at 100 μm). This enormous kinetic inductance is a critical disadvantage of CNTs for high-frequency operation.

## 4.3 Capacitance Comparison (fF)

### Length = 100 μm

| Node | Cu C (fF) | CNT C (fF) | CNT/Cu Ratio |
| --- | --- | --- | --- |
| 45 nm | 3.28 | 17.36 | 5.3× |
| 22 nm | 2.80 | 15.12 | 5.4× |
| 14 nm | 2.46 | 13.56 | 5.5× |
| 7 nm | 2.16 | 11.99 | 5.6× |

### Length = 500 μm

| Node | Cu C (fF) | CNT C (fF) | CNT/Cu Ratio |
| --- | --- | --- | --- |
| 45 nm | 16.41 | 86.80 | 5.3× |
| 22 nm | 14.01 | 75.58 | 5.4× |
| 14 nm | 12.32 | 67.81 | 5.5× |
| 7 nm | 10.79 | 59.95 | 5.6× |

### Length = 1000 μm

| Node | Cu C (fF) | CNT C (fF) | CNT/Cu Ratio |
| --- | --- | --- | --- |
| 45 nm | 32.83 | 173.61 | 5.3× |
| 22 nm | 28.01 | 151.16 | 5.4× |
| 14 nm | 24.64 | 135.62 | 5.5× |
| 7 nm | 21.59 | 119.89 | 5.6× |

NOTE CNT capacitance is ~5.3–5.6× higher than Cu across all nodes and lengths. This is largely due to the quantum capacitance contribution which is an intrinsic property of 1D conductors. Cu capacitance benefits from node scaling (smaller W/H reduces fringe capacitance). CNT capacitance scales less favorably due to the fixed quantum capacitance per channel.

# 5. RC Time Constant Analysis (τ = R × C)

| Node | Length | Cu τ (ps) | CNT τ (ps) | CNT/Cu Ratio |
| --- | --- | --- | --- | --- |
| 45nm | 100 μm | 2.88 | 763.6 | 265× |
| 45nm | 500 μm | 72.0 | 19,074 | 265× |
| 45nm | 1000 μm | 288 | 76,297 | 265× |
| 14nm | 100 μm | 68.9 | 2,832 | 41.1× |
| 14nm | 500 μm | 1,725 | 70,726 | 41.0× |
| 14nm | 1000 μm | 6,900 | 282,904 | 41.0× |
| 7nm | 100 μm | 559 | 6,571 | 11.8× |
| 7nm | 500 μm | 13,972 | 164,145 | 11.7× |
| 7nm | 1000 μm | 55,887 | 656,291 | 11.7× |

Key Insight: The RC time constant ratio shrinks dramatically from 265× at 45 nm to 11.8× at 7 nm, driven entirely by Cu's rapidly escalating R. At 7 nm, Cu's 10× resistivity increase nearly closes the gap. Cu is still faster, but the performance lead is eroding.

# 6. Circuit-Level Simulation Results

## 6.1 CMOS Inverter Chain — Propagation Delay Summary

Two-stage 90nm CMOS inverter chain; only the interconnect node uses scaled Cu/CNT parameters

### 45nm Node Interconnect

| Length | Circuit | Material | Approx. Delay (50% crossing) | Timescale |
| --- | --- | --- | --- | --- |
| 100 μm | Inverter Chain | Cu | ~5.5 ns | ns range |
| 100 μm | Inverter Chain | CNT | ~11.5 ns | ns range |
| 500 μm | Inverter Chain | Cu | ~4.7 ns | ns range |
| 500 μm | Inverter Chain | CNT | ~169 ns | 100s ns |
| 1000 μm | Inverter Chain | Cu | ~3.7 ns | ns range |
| 1000 μm | Inverter Chain | CNT | ~450 ns | 100s ns |

IMPORTANT At 45nm / 1000μm, CNT delay (~450 ns) is ~120× slower than Cu (~3.7 ns). This is the worst-case scenario because 45nm has the largest CNT bundle (N_m=299) which still results in high total resistance due to R_Q, while Cu operates near its bulk resistivity.

### 14nm Node Interconnect

| Length | Circuit | Material | Approx. Delay | Key Notes |
| --- | --- | --- | --- | --- |
| 100 μm | Inverter Chain | Cu | ~5.8 ns | Rising Cu R begins |
| 100 μm | Inverter Chain | CNT | ~59 ns | R_Q dominated |
| 500 μm | Inverter Chain | Cu | ~33 ns | R*C ~1.7 ns |
| 500 μm | Inverter Chain | CNT | ~0.75 μs | 22× slower |
| 1000 μm | Inverter Chain | Cu | ~114 ns | R scales 10× |
| 1000 μm | Inverter Chain | CNT | ~6.3 μs | 55× slower |

### 7nm Node Interconnect

| Length | Circuit | Material | Approx. Delay | Key Notes |
| --- | --- | --- | --- | --- |
| 100 μm | Inverter Chain | Cu | ~13.8 ns | Cu R is ~259 kΩ! |
| 100 μm | Inverter Chain | CNT | ~89 ns | Only 6.5× slower |
| 500 μm | Inverter Chain | Cu | ~960 ns | Cu τ ~14 ns |
| 500 μm | Inverter Chain | CNT | ~3.5 μs | 3.6× slower |
| 1000 μm | Inverter Chain | Cu | ~3.48 μs | Cu comparable to CNT |
| 1000 μm | Inverter Chain | CNT | ~10.87 μs | Only ~3× slower |

IMPORTANT At 7nm / 1000μm, both Cu and CNT have delays in the microsecond range. This represents a fundamental interconnect bottleneck — neither material provides fast signal propagation at this technology node for long interconnects.

## 6.2 4-Bit Ripple-Carry Adder (RCA) — Signal Integrity Summary

Worst-case ripple delay across 3 cascaded carry segments

### 45nm Node — RCA Results

| Length | Material | Carry Propagation Time | Signal Quality |
| --- | --- | --- | --- |
| 100 μm | Cu | ~11.8 ns | Clean, sharp transitions |
| 100 μm | CNT | ~10.9 ns | Clean, slight RC rounding |
| 500 μm | Cu | ~6.5 ns per bit | Good digital margins |
| 500 μm | CNT | ~89 ns per bit | Visible slowing |
| 1000 μm | Cu | ~6.5 ns | V(n_c1_raw) reaches 1.3V |
| 1000 μm | CNT | ~286 μs | Severely degraded |

CAUTION The 45nm / 1000μm CNT RCA waveform (page 1 of PDF) shows a stimulus period of ~656 ns (100× the 100μm CNT RCA) confirming the R*C per segment ~−656 ns. The output V(sum) barely reaches full swing before the next clock edge — severe hold time violation.

### 14nm Node — RCA Results

| Length | Material | Carry Time | Ripple Delay | Signal Notes |
| --- | --- | --- | --- | --- |
| 100 μm | Cu | ~18 ns | ~12 ns worst-case | Clean square waves |
| 100 μm | CNT (R=1,042,870Ω!) | ~660 ns |  | Over-damped oscillation |
| 500 μm | Cu | ~33 ns | ~17 ns | Still recognizable |
| 500 μm | CNT (R=1,042,870Ω) | ~53.7 ns |  | Severely distorted |
| 1000 μm | Cu | ~26 ns | ~21 ns | Degraded but ok |
| 1000 μm | CNT (R=2,085,479Ω) | ~66 ns |  | Completely distorted |

WARNING The 14nm / 1000μm CNT RCA waveform (page 7) shows completely saturated/distorted waveforms — the V(n_c1_raw) signal is essentially a sawtooth wave. The CNT bundle resistance of 2.085 MΩ causes such high RC loading that the carry chain can never settle properly. This is functionally broken for digital logic at this combination.

### 7nm Node — RCA Results

| Length | Material | Timing | Observation |
| --- | --- | --- | --- |
| 100 μm | Cu | ~24.6 ns | Degraded edges but functional |
| 100 μm | CNT | ~660 ns | High resistance, slow |
| 500 μm | Cu | ~708 ns | Near marginal |
| 500 μm | CNT | ~8.4 μs | 12× slower than Cu |
| 1000 μm | Cu | ~3.48 μs | Comparable to CNT! |
| 1000 μm | CNT | ~60.5 μs | Still ~17× slower |

# 7. Scaling Trends: How R, L, C Vary with Length

## 7.1 Resistance vs. Length (at 7nm Node)

| Length | Cu R (Ω) | Growth Factor | CNT R (Ω) | Growth Factor |
| --- | --- | --- | --- | --- |
| 100 μm | 258,858 | 1× | 548,055 | 1× |
| 500 μm | 1,294,291 | 5.0× | 2,737,535 | 5.0× |
| 1000 μm | 2,588,583 | 10.0× | 5,474,384 | 9.99× |

Both Cu and CNT resistance scale linearly with length. This is expected: Cu because ρ is length-independent (R = ρL/A); CNT because the scattering term R_Q*(L/λ_eff) dominates at 100 μm+ (λ_eff = 49 nm << 100 μm).

## 7.2 Resistance vs. Node (at 1000 μm Length)

| Node | Cu R (kΩ) | Growth Factor | CNT R (kΩ) | Growth Factor |
| --- | --- | --- | --- | --- |
| 45nm | 8.78 | 1× | 439.4 | 1× |
| 22nm | 49.5 | 5.6× | 1,123 | 2.6× |
| 14nm | 280.1 | 31.9× | 2,085 | 4.7× |
| 7nm | 2,589 | 295× | 5,474 | 12.5× |

Key Insight: Cu resistance scales 295× from 45nm to 7nm (at 1 mm length), while CNT resistance scales only 12.5×. This demonstrates CNT's superior node scaling. The CNT R scaling is limited by shrinking bundle size (fewer N_m), while Cu scaling is dominated by exponentially rising ρ_eff.

# 8. Material-Level Physical Insights

## 8.1 Why Cu Gets Worse at Smaller Nodes

45nm: ρ_eff = 2.43 μΩ·cm (only 45% above bulk) → Surface scattering mild (W=38nm >> λ_Cu≈40nm) → Grain boundaries: α=0.17 (sub-linear regime) 14nm: ρ_eff = 7.73 μΩ·cm (4.6× bulk) → W_eff = 11nm << λ_Cu: STRONG surface scattering → α=0.55: deep into grain-boundary saturation → BOTH mechanisms simultaneously degrading 7nm: ρ_eff = 16.83 μΩ·cm (10× bulk) → W_eff = 5nm: nearly one scattering mean-free path → Specularity essentially zero at sub-10nm → ρ_MS multiplier = 2.51: grain boundaries add 2.5× on top → CATASTROPHIC compounding of both effects

## 8.2 Why CNT Is Better at Smaller Nodes (But Still Worse Absolutely)

CNT resistance scales as: R_total = (R_Q + R_Q*(L/λ_eff) + R_contact) / N_m At 100 μm: R_Q*(L/λ_eff) = 6453 * (100,000/49.1) = 13.1 MΩ (per CNT) This FIXED scattering term dominates → bundle resistance ∝ 1/N_m As node shrinks: N_m decreases (from 299 → 24), so R ∝ 1/N_m increases BUT: The scattering term (λ_eff) does NOT change with node (phonon-limited) → CNT resistance scales only as geometric packing changes (mild) vs Cu whose ρ_eff doubles/triples with every node step

## 8.3 Crossover Analysis: When Does CNT Become Competitive?

| Node | Length for R_Cu = R_CNT | Status |
| --- | --- | --- |
| 45nm | >> 10 mm | Cu always better |
| 22nm | ~10 mm | Cu better for chip scale |
| 14nm | ~2.5 mm | Cu better but gap closing |
| 7nm | ~400 μm | Near-competitive at 500 μm! |

TIP At 7nm node with ~400 μm interconnect length, Cu and CNT resistances become approximately equal. For longer global interconnects (>1 mm) at 7nm, CNT bundles would theoretically offer lower resistance if contact resistance can be reduced. The current bottleneck is R_contact (included in R_Q term), which can be improved with better fabrication.

# 9. Waveform Analysis from Simulation PDF

## 9.1 Inverter Chain: Transition Quality

| Condition | Cu Waveform | CNT Waveform |
| --- | --- | --- |
| 45nm/100μm | Sharp, fast rise/fall (~2–3 ns) | Slightly slower rise, ~10–12 ns |
| 45nm/500μm | Very fast transition, few ns | ~170 ns, still functional |
| 45nm/1000μm | Fast, ~3.7 ns delay | ~450 ns, highly distorted |
| 7nm/100μm | Slow but OK (~13.8 ns) | Very slow (~89 ns) |
| 7nm/500μm | ~960 ns, marginal | ~3.5 μs, barely functional |
| 7nm/1000μm | ~3.48 μs (Cu bottlenecked!) | ~10.87 μs, unusable for GHz |

## 9.2 RCA: Signal Integrity

The ripple-carry adder simulations reveal important behavior:

- Cu @ 14nm/100μm (page 10): Clean bit transitions; carry-chain output V(sum) shows proper logic levels. Worst-case carry ~18 ns.

- CNT @ 14nm/100μm (page 5): V(n_c1_raw) shows massively distorted waveform — the signal appears as a triangular/sinusoidal shape rather than square pulses, indicating the CNT RC constant (~208 kΩ × 13.6 fF = ~2.83 ns × 100 stages ≈ microseconds for full adder) prevents proper settling.

- Cu @ 7nm/1000μm (page 1): Operating at ~3.48 μs period — this is essentially slow serial operation, not the intended parallel digital speed.

- CNT @ 7nm/1000μm (page 1): Parameters visible: r_int = 5,474,383.56 Ω, c_int = 119.89 fF, l_int = 336.43 nH — the RCA is marginally functional with stimulus periods of ~656 ns (100× the 100μm Cu case).

# 10. Summary Comparison Tables

## 10.1 R Ratio (CNT/Cu) — How Many Times More Resistant is CNT?

| Node | 100 μm | 500 μm | 1000 μm |
| --- | --- | --- | --- |
| 45nm | 50.1× | 50.1× | 50.1× |
| 22nm | 22.7× | 22.7× | 22.7× |
| 14nm | 7.5× | 7.4× | 7.5× |
| 7nm | 2.1× | 2.1× | 2.1× |

CNT resistance is relatively independent of length (same ratio at all lengths due to shared R_Q domination)

## 10.2 C Ratio (CNT/Cu) — How Many Times More Capacitive is CNT?

| Node | 100 μm | 500 μm | 1000 μm |
| --- | --- | --- | --- |
| 45nm | 5.3× | 5.3× | 5.3× |
| 22nm | 5.4× | 5.4× | 5.4× |
| 14nm | 5.5× | 5.5× | 5.5× |
| 7nm | 5.6× | 5.6× | 5.6× |

Consistent ~5.3–5.6× across all conditions — quantum capacitance adds a fixed per-channel overhead

## 10.3 L Ratio (CNT/Cu) — How Many Times More Inductive is CNT?

| Node | 100 μm | 500 μm | 1000 μm |
| --- | --- | --- | --- |
| 45nm | 17× | 14× | 13× |
| 22nm | 40× | 34× | 32× |
| 14nm | 71× | 60× | 57× |
| 7nm | 174× | 149× | 141× |

Kinetic inductance grows inverse to N_m — smaller nodes with fewer metallic CNTs have enormous L

# 11. Key Takeaways & Engineering Implications

## Copper Strengths

- Low resistance at 45nm: Only 878 Ω at 100 μm — excellent for short local interconnects

- Very low capacitance: 3.28 fF at 100 μm — minimal RC loading on drivers

- Negligible inductance: Sub-nH values, no kinetic inductance overhead

- Proven manufacturability at all nodes

## Copper Weaknesses

- Catastrophic resistivity at 7nm: 10× above bulk — R = 2.59 MΩ at 1 mm

- Non-linear scaling: 295× resistance increase from 45nm → 7nm at 1 mm

- Electromigration risk intensifies at sub-10nm dimensions

- Barrier metal overhead: At 7nm, barrier takes 29% of width (2×1 nm barrier on 7nm wire)

## CNT Strengths

- Favorable node scaling: Only 12.5× resistance increase from 45nm → 7nm (vs Cu's 295×)

- Near-competitive at 7nm: Only 2.1× higher R than Cu — approaching viable range

- Better high-current capacity: Each CNT rated for ~25 μA → bundle handles high current density

- No electromigration: Covalent C-C bonds prevent metal migration

- Capacitance scales down with node (smaller bundles, lower C_E)

## CNT Weaknesses

- Enormous quantum+contact resistance at short lengths: At 100 μm / 45nm: 50× higher R than Cu

- Massive kinetic inductance: 174× higher than Cu at 7nm/100μm — problematic for GHz

- ~5.5× higher capacitance: Quantum capacitance adds unavoidable overhead

- Fabrication challenges: Controlling metallic fraction F_m = 1/3 and bundle density remains difficult

# 12. Conclusions

## The Core Trade-off

The study reveals a fundamental material crossover behavior that is technology-node dependent:

At 45nm: Cu is dominant — 50× lower R, suitable for all interconnect lengths At 22nm: Cu still dominant but gap narrowing — 22.7× lower R At 14nm: Cu still better, but only 7.5× — Cu viability window shrinking fast At 7nm: Cu barely better — only 2.1× lower R, both are problematic at mm scales

## The Contact Resistance Bottleneck

The single biggest limitation for CNTs is the R_Q = 6,453 Ω per CNT quantum/contact resistance. This is a fixed overhead that:

- Makes short CNT bundles extremely resistive (~44 kΩ at 100 μm / 45nm)

- Cannot be removed without fundamental changes to quantum mechanics

- Can however be partially mitigated by better contacts (reducing R_contact = 0 assumed here — actual fabricated contacts add additional resistance)

- Scales favorably with length: at 1 mm, scattering dominates and quantum overhead is relatively smaller

## Outlook for VLSI

- Near-term (7nm, 5nm): Cu with cobalt/ruthenium barrier metals remains the only practical option for local/intermediate interconnects

- Medium-term: CNT bundles with sorted metallic CNTs (F_m → 1.0) could reduce resistance 3× and become viable for global interconnects >500 μm at 7nm

- Long-term: At sub-5nm nodes, Cu's resistivity may exceed CNT's — the crossover is real and imminent

- The RC Product: Even if CNT R matches Cu R at 7nm, the 5.5× higher CNT capacitance means RC delay is still worse — both R and C must be optimized simultaneously

Analysis based on: LTSpice simulation results (interconnect.pdf, 18 pages), RLC parameters (CNT_Cu_RLC_Calculations_corrected.xlsx), models from Fuchs-Sondheimer, Mayadas-Shatzkes, Sakurai-Tamaru, and SWCNT interconnect literature.