# Results and Discussion

Copper vs. Single-Walled Carbon Nanotube (SWCNT) Bundle Interconnects at the 45 nm, 22 nm, 14 nm, and 7 nm Technology Nodes

## 1. Technology Node Geometry and Copper Resistivity Scaling

Four technology nodes — 45 nm, 22 nm, 14 nm, and 7 nm — were evaluated, each with its own copper wire cross-section and carbon-nanotube bundle geometry (Table 1). Because a diffusion barrier of fixed thickness must be reserved on every sidewall of the copper trench, the effective conducting cross-section shrinks faster than the drawn wire dimensions: at 7 nm only 5 nm of width remains available for current flow, versus 38 nm at 45 nm. The SWCNT bundle experiences an analogous effect — the number of tubes that physically fit in the same footprint, and the number of those that are metallic (roughly one in three), falls from 299 metallic tubes at 45 nm to just 24 at 7 nm.

| Node | W (nm) | H (nm) | W_eff,Cu (nm) | H_eff,Cu (nm) | N_total (CNT) | N_metallic (CNT) |
| --- | --- | --- | --- | --- | --- | --- |
| 45 nm | 45 | 90 | 38 | 73 | 897 | 299 |
| 22 nm | 22 | 45 | 18 | 37.6 | 350 | 117 |
| 14 nm | 14 | 28 | 11 | 25.1 | 190 | 63 |
| 7 nm | 7 | 14 | 5 | 13 | 72 | 24 |

Table 1. Drawn and effective wire/bundle geometry at each technology node.

Copper's size-effect-corrected resistivity (ρ_eff), combining Fuchs–Sondheimer surface scattering with Mayadas–Shatzkes grain-boundary scattering, degrades sharply and non-linearly as the node shrinks (Table 2). Relative to bulk copper (1.68 μΩ·cm), ρ_eff is only 1.45× higher at 45 nm but reaches 10.02× bulk at 7 nm. The escalation roughly doubles again between 14 nm and 7 nm, reflecting the simultaneous intensification of both scattering mechanisms: the surface-scattering multiplier nearly quadruples (1.16→3.98) while the grain-boundary multiplier grows 2.5-fold (1.25→2.51) over the same range.

| Node | ρ_FS Multiplier | ρ_MS Multiplier | ρ_eff (μΩ·cm) | vs. Bulk Cu (1.68 μΩ·cm) |
| --- | --- | --- | --- | --- |
| 45 nm | 1.163 | 1.247 | 2.43 | 1.45× |
| 22 nm | 1.332 | 1.495 | 3.35 | 2.00× |
| 14 nm | 2.601 | 1.769 | 7.73 | 4.60× |
| 7 nm | 3.984 | 2.514 | 16.83 | 10.02× |

Table 2. Copper effective resistivity scaling due to combined surface and grain-boundary scattering.

## 2. Resistance, Inductance, and Capacitance: Copper vs. SWCNT Bundles

### 2.1 Resistance

Extracted resistance values for interconnect lengths of 100 μm, 500 μm, and 1000 μm are summarized in Table 3. At every node the CNT/Cu resistance ratio is essentially independent of wire length, because the bundle resistance is dominated by the fixed quantum resistance (R_Q = h/4e² ≈ 6,453 Ω per tube) and contact resistance rather than by the length-dependent scattering term. What does change with node is the ratio itself: it falls steadily from 50.1× at 45 nm to 22.7× at 22 nm, 7.4–7.5× at 14 nm, and just 2.1× at 7 nm — copper's own resistivity blow-up is closing the gap far more than any improvement in the CNT bundle itself.

| Node | Length (μm) | Cu R (Ω) | CNT R (Ω) | CNT/Cu Ratio |
| --- | --- | --- | --- | --- |
| 45 nm | 100 | 877.7 | 43,991 | 50.1× |
| 45 nm | 500 | 4,389 | 219,735 | 50.1× |
| 45 nm | 1000 | 8,777 | 439,415 | 50.1× |
| 22 nm | 100 | 4,946 | 112,422 | 22.7× |
| 22 nm | 500 | 24,730 | 561,546 | 22.7× |
| 22 nm | 1000 | 49,461 | 1,122,950 | 22.7× |
| 14 nm | 100 | 28,006 | 208,783 | 7.5× |
| 14 nm | 500 | 140,028 | 1,042,870 | 7.4× |
| 14 nm | 1000 | 280,057 | 2,085,479 | 7.5× |
| 7 nm | 100 | 258,858 | 548,055 | 2.1× |
| 7 nm | 500 | 1,294,291 | 2,737,535 | 2.1× |
| 7 nm | 1000 | 2,588,583 | 5,474,384 | 2.1× |

Table 3. Total interconnect resistance, copper vs. SWCNT bundle, across node and length.

### 2.2 Inductance

CNT inductance is dominated by kinetic inductance rather than the conventional magnetic inductance that governs copper (Table 4). Because kinetic inductance scales inversely with the number of metallic tubes in the bundle, the CNT/Cu ratio grows sharply as the node shrinks and N_metallic falls — from roughly 13–17× at 45 nm to 141–174× at 7 nm. This trend runs in the opposite direction from the resistance trend: copper's magnetic inductance stays comparatively flat with node scaling (0.16–0.19 nH at 100 μm), so as CNTs become more resistance-competitive at smaller nodes, their inductance disadvantage simultaneously worsens — a genuine trade-off rather than a uniform improvement.

| Node | Length (μm) | Cu L (nH) | CNT L (nH) | CNT/Cu Ratio |
| --- | --- | --- | --- | --- |
| 45 nm | 100 | 0.158 | 2.727 | 17.2× |
| 45 nm | 500 | 0.952 | 13.637 | 14.3× |
| 45 nm | 1000 | 2.042 | 27.275 | 13.4× |
| 22 nm | 100 | 0.172 | 6.925 | 40.3× |
| 22 nm | 500 | 1.019 | 34.625 | 34.0× |
| 22 nm | 1000 | 2.178 | 69.250 | 31.8× |
| 14 nm | 100 | 0.180 | 12.835 | 71.3× |
| 14 nm | 500 | 1.061 | 64.177 | 60.5× |
| 14 nm | 1000 | 2.261 | 128.353 | 56.8× |
| 7 nm | 100 | 0.193 | 33.643 | 174.3× |
| 7 nm | 500 | 1.127 | 168.213 | 149.3× |
| 7 nm | 1000 | 2.393 | 336.426 | 140.6× |

Table 4. Total interconnect inductance, copper vs. SWCNT bundle, across node and length.

### 2.3 Capacitance

Capacitance shows the most consistent trend of the three parameters (Table 5): the CNT bundle is 5.3–5.6× more capacitive than copper at every node and length studied, a gap that widens only marginally as the node shrinks. This is attributable to quantum capacitance, an intrinsic per-channel property of one-dimensional conductors that does not shrink away with geometric scaling. Copper capacitance, by contrast, benefits directly from node scaling — smaller wire cross-sections reduce fringe-field coupling to neighboring wires — so the absolute capacitance gap actually narrows slightly at smaller nodes even as the ratio edges upward.

| Node | Length (μm) | Cu C (fF) | CNT C (fF) | CNT/Cu Ratio |
| --- | --- | --- | --- | --- |
| 45 nm | 100 | 3.28 | 17.36 | 5.3× |
| 45 nm | 500 | 16.41 | 86.80 | 5.3× |
| 45 nm | 1000 | 32.83 | 173.61 | 5.3× |
| 22 nm | 100 | 2.80 | 15.12 | 5.4× |
| 22 nm | 500 | 14.01 | 75.58 | 5.4× |
| 22 nm | 1000 | 28.01 | 151.16 | 5.4× |
| 14 nm | 100 | 2.46 | 13.56 | 5.5× |
| 14 nm | 500 | 12.32 | 67.81 | 5.5× |
| 14 nm | 1000 | 24.64 | 135.62 | 5.5× |
| 7 nm | 100 | 2.16 | 11.99 | 5.6× |
| 7 nm | 500 | 10.79 | 59.95 | 5.6× |
| 7 nm | 1000 | 21.59 | 119.89 | 5.6× |

Table 5. Total interconnect capacitance, copper vs. SWCNT bundle, across node and length.

## 3. RC Time Constant Analysis

The RC product (τ = R × C) captures the combined effect of the resistance and capacitance trends above, and is the dominant driver of the propagation delays observed in the circuit-level simulations discussed in Section 4 (Table 6). The CNT/Cu τ ratio shrinks dramatically — from about 265× at 45 nm to roughly 41× at 14 nm and 11.7–11.8× at 7 nm — almost entirely because copper's resistance degrades so rapidly at advanced nodes, not because the CNT bundle itself improves. Copper remains the faster interconnect in every case studied, but its performance lead over CNTs erodes by more than an order of magnitude across the 45-to-7 nm range.

| Node | Length (μm) | Cu τ (ps) | CNT τ (ps) | CNT/Cu Ratio |
| --- | --- | --- | --- | --- |
| 45 nm | 100 | 2.88 | 763.6 | 265× |
| 45 nm | 500 | 72.0 | 19,074 | 265× |
| 45 nm | 1000 | 288 | 76,297 | 265× |
| 14 nm | 100 | 68.9 | 2,832 | 41.1× |
| 14 nm | 500 | 1,725 | 70,726 | 41.0× |
| 14 nm | 1000 | 6,900 | 282,904 | 41.0× |
| 7 nm | 100 | 559 | 6,571 | 11.8× |
| 7 nm | 500 | 13,972 | 164,145 | 11.7× |
| 7 nm | 1000 | 55,887 | 656,291 | 11.7× |

Table 6. RC time constant, copper vs. SWCNT bundle, at 45 nm, 14 nm, and 7 nm.

## 4. Circuit-Level Simulation Results

Extracted R, L, and C values were embedded as LTspice parameters and exercised in two test circuits at fixed 90 nm CMOS device sizing, so that any change in delay or signal quality is attributable to the interconnect alone: a two-stage inverter chain, which isolates the wire's own contribution to propagation delay, and a 4-bit ripple-carry adder (RCA), in which the interconnect is inserted into the internal carry chain so that delay accumulates across three cascaded segments.

### 4.1 CMOS Inverter Chain — Propagation Delay

Table 7 reports the approximate 50%-crossing propagation delay for each node/length/material combination. The worst relative case occurs at 45 nm/1000 μm, where the CNT delay (≈450 ns) is roughly 120× slower than copper (≈3.7 ns) — the 45 nm bundle has the largest number of metallic tubes of any node studied, yet its resistance is still overwhelmingly dominated by the fixed quantum/contact term. At the opposite extreme, at 7 nm/1000 μm both materials fall into the microsecond range (≈3.48 μs for Cu, ≈10.87 μs for CNT), indicating a fundamental interconnect bottleneck at this combination of node and length that neither material resolves.

| Node | Length (μm) | Cu Delay (≈50%) | CNT Delay (≈50%) |
| --- | --- | --- | --- |
| 45 nm | 100 | ~5.5 ns | ~11.5 ns |
| 45 nm | 500 | ~4.7 ns | ~169 ns |
| 45 nm | 1000 | ~3.7 ns | ~450 ns |
| 14 nm | 100 | ~5.8 ns | ~59 ns |
| 14 nm | 500 | ~33 ns | ~0.75 μs |
| 14 nm | 1000 | ~114 ns | ~6.3 μs |
| 7 nm | 100 | ~13.8 ns | ~89 ns |
| 7 nm | 500 | ~960 ns | ~3.5 μs |
| 7 nm | 1000 | ~3.48 μs | ~10.87 μs |

Table 7. Two-stage CMOS inverter-chain propagation delay, 90 nm devices with scaled Cu/CNT interconnect.

### 4.2 4-Bit Ripple-Carry Adder — Signal Integrity

The RCA results (Table 8) show that the resistance and capacitance penalties of the CNT bundle translate directly into degraded logic-level signal quality, not just added delay. At 14 nm/100 μm, the CNT carry-chain node exhibits an over-damped, rounded transition rather than a clean digital edge; at 14 nm/1000 μm (bundle resistance ≈ 2.09 MΩ) the internal carry waveform becomes essentially a sawtooth rather than a square pulse, a condition that is functionally broken for reliable digital logic. Because the RCA cascades three interconnect segments back-to-back on the carry path, these per-segment RC penalties compound: stimulus periods across the nine node/length cases had to be stretched from tens of nanoseconds up to roughly 656 ns (45 nm/1000 μm CNT) and beyond simply to allow the cascaded chain time to settle, illustrating that system-level (multi-segment) delay degrades faster than the single-wire RC estimates in Sections 2–3 would suggest on their own.

| Node | Length (μm) | Cu Carry Time | CNT Carry Time | Signal Quality |
| --- | --- | --- | --- | --- |
| 45 nm | 100 | ~11.8 ns | ~10.9 ns | Both clean |
| 45 nm | 500 | ~6.5 ns/bit | ~89 ns/bit | CNT visibly slowed |
| 45 nm | 1000 | ~6.5 ns | ~286 μs | CNT severely degraded |
| 14 nm | 100 | ~18 ns | ~660 ns | CNT over-damped |
| 14 nm | 500 | ~33 ns | ~53.7 ns | CNT distorted |
| 14 nm | 1000 | ~26 ns | ~66 ns | CNT sawtooth / broken |
| 7 nm | 100 | ~24.6 ns | ~660 ns | Cu degraded, functional |
| 7 nm | 500 | ~708 ns | ~8.4 μs | CNT ~12× slower |
| 7 nm | 1000 | ~3.48 μs | ~60.5 μs | Both marginal |

Table 8. Ripple-carry-adder carry-chain propagation time and qualitative signal quality, 90 nm logic with scaled interconnect.

## 5. Scaling Trends: Length and Node Dependence

At a fixed node, both materials' resistance scales essentially linearly with interconnect length (Table 9): copper because ρ is length-independent (R = ρL/A), and the CNT bundle because the phonon-scattering term R_Q·(L/λ_eff) already dominates over the fixed quantum/contact resistance once length exceeds λ_eff ≈ 49 nm, so growth is likewise proportional to L.

| Length (μm) | Cu R (Ω) | Growth | CNT R (Ω) | Growth |
| --- | --- | --- | --- | --- |
| 100 | 258,858 | 1× | 548,055 | 1× |
| 500 | 1,294,291 | 5.0× | 2,737,535 | 5.0× |
| 1000 | 2,588,583 | 10.0× | 5,474,384 | 9.99× |

Table 9. Resistance vs. interconnect length at the 7 nm node.

At a fixed length, however, the two materials scale very differently with technology node (Table 10). From 45 nm to 7 nm, copper resistance grows 295× at 1000 μm, driven by the exponential-like rise in ρ_eff documented in Section 1. Over the same range, CNT bundle resistance grows only 12.5×, because its scaling is governed by the shrinking bundle population (N_metallic falling from 299 to 24) rather than by any node-dependent change in the scattering physics — the phonon mean free path λ_eff is fixed regardless of node. This asymmetry is the central reason the CNT/Cu resistance ratio narrows so much between 45 nm and 7 nm even though the CNT bundle itself is not improving in any absolute sense.

| Node | Cu R (kΩ) | Growth | CNT R (kΩ) | Growth |
| --- | --- | --- | --- | --- |
| 45 nm | 8.78 | 1× | 439.4 | 1× |
| 22 nm | 49.5 | 5.6× | 1,123 | 2.6× |
| 14 nm | 280.1 | 31.9× | 2,085 | 4.7× |
| 7 nm | 2,589 | 295× | 5,474 | 12.5× |

Table 10. Resistance vs. technology node at a fixed interconnect length of 1000 μm.

## 6. Crossover Analysis

Combining the length- and node-scaling behavior above identifies the approximate interconnect length at which copper and CNT-bundle resistance become equal at each node (Table 11). At 45 nm the crossover length is far beyond any practical on-chip interconnect (>>10 mm), so copper is unconditionally preferred. The crossover length shrinks steadily with node — to roughly 10 mm at 22 nm, 2.5 mm at 14 nm, and only about 400 μm at 7 nm — to the point that at 7 nm the two materials are nearly resistance-matched around 400–500 μm, squarely within the range of practical intermediate/global interconnect lengths. Whether this near-parity translates into an actual CNT advantage for longer 7 nm interconnects depends heavily on reducing the contact resistance folded into the R_Q term, which was held fixed in this analysis (R_contact assumed negligible/zero) and represents the largest remaining source of uncertainty in the comparison.

| Node | Length for R_Cu ≈ R_CNT | Status |
| --- | --- | --- |
| 45 nm | >> 10 mm | Cu always better |
| 22 nm | ~10 mm | Cu better for chip scale |
| 14 nm | ~2.5 mm | Cu better, gap narrowing |
| 7 nm | ~400 μm | Near-competitive at 500 μm |

Table 11. Approximate interconnect length at which copper and CNT-bundle resistance converge, by node.

## 7. Discussion

### 7.1 Physical Origins of Copper's Degradation at Advanced Nodes

Copper's resistivity blow-up follows directly from the two scattering mechanisms compounding as the effective wire width shrinks toward and below copper's electron mean free path (λ_Cu ≈ 40 nm). At 45 nm, the effective width (38 nm) is still comparable to λ_Cu, surface scattering is mild, and the grain-boundary parameter α (≈0.17) sits in a sub-linear regime, so ρ_eff is only 45% above bulk. By 14 nm, the effective width (11 nm) is well below λ_Cu, surface scattering becomes strong, and α (≈0.55) moves deep into the grain-boundary-saturation regime, so both mechanisms degrade resistivity simultaneously and ρ_eff reaches 4.6× bulk. At 7 nm the effective width (5 nm) is comparable to a single scattering mean free path, surface specularity is effectively zero, and the grain-boundary multiplier alone adds another 2.5× on top — the two effects compound rather than simply add, producing the observed 10×-bulk resistivity.

### 7.2 Physical Origins of CNT Bundle Behavior

The CNT bundle's total resistance can be written as R_total = (R_Q + R_Q·(L/λ_eff) + R_contact) / N_metallic. At interconnect lengths of 100 μm and above, the scattering term R_Q·(L/λ_eff) (≈13.1 MΩ per tube at 100 μm) dominates the numerator and is essentially fixed by phonon physics — it does not change with technology node. What does change with node is N_metallic, which falls from 299 to 24 across the nodes studied, so the bundle's resistance scales only through this geometric packing factor. This is the mechanistic reason CNT resistance scales far more mildly with node (12.5× from 45 to 7 nm) than copper's scattering-driven resistivity (295× over the same range): the CNT penalty is architectural (how many tubes fit and conduct), not a fundamental materials degradation.

### 7.3 Trade-offs and Engineering Implications

Taken together, the results point to a technology-node-dependent crossover rather than a universal winner. At 45 nm and 22 nm, copper's resistance advantage (50× and 23×) is overwhelming and copper remains the clear choice for essentially all interconnect lengths. At 14 nm the copper advantage has fallen to 7–8× and continues to erode. At 7 nm, copper's resistance advantage has collapsed to only 2.1×, and for interconnects longer than roughly 400–500 μm the two materials are approximately resistance-matched — even though copper still wins decisively on inductance (140–174× lower at 7 nm) and capacitance (5.6× lower), and retains a mature, well-understood manufacturing process.

CNT bundles' principal liabilities are not resistive in nature at advanced nodes but reactive: kinetic inductance 140–174× higher than copper's magnetic inductance at 7 nm, and quantum capacitance that keeps total capacitance 5.3–5.6× higher across every node and length studied. Both are intrinsic, quantum-mechanical properties of one-dimensional conduction and cannot be engineered away the way copper's electromigration or barrier-thickness problems can — they can only be diluted by increasing the number of metallic tubes in a bundle (raising N_metallic and the metallic fraction F_m, nominally ≈1/3 in this study), which is itself a difficult fabrication and sorting problem. The RCA results reinforce that these penalties are not merely a delay inconvenience: at several node/length combinations (notably 14 nm at longer lengths) the CNT interconnect's RC loading was severe enough to distort the carry-chain waveform into a non-digital, sawtooth-like signal, a signal-integrity failure mode that copper did not exhibit at any node or length studied.

For near-term nodes (7 nm and below), copper — typically paired with cobalt or ruthenium barrier/liner metals to recover some of the effective cross-section lost to a pure tantalum-nitride barrier — remains the more practical choice for local and intermediate interconnects, where its inductance and capacitance advantages continue to dominate overall RC delay despite its degraded resistivity. CNT bundles are most credible as a medium-term candidate for global interconnects longer than about 500 μm at 7 nm and below, and specifically contingent on reducing the metal–nanotube contact resistance folded into R_Q and on improving the sorted metallic fraction toward F_m → 1, either of which could reduce bundle resistance several-fold. Even so, because RC delay depends on both terms, matching or beating copper's resistance alone would not be sufficient: the 5.3–5.6× capacitance penalty means resistance and capacitance must be improved together for CNT interconnects to offer a genuine delay advantage rather than merely a resistance advantage.

Data sources: RLC parameters extracted from CNT_Cu_RLC_Calculations_corrected.xlsx (Summary sheet); circuit-level delay and waveform behavior extracted from LTspice transient simulations (interconnect.pdf, 18 pages) of a two-stage 90 nm CMOS inverter chain and a 4-bit ripple-carry adder.