RLC Modeling Formula Reference

CNT Bundle vs Copper Interconnects  |  Technology Nodes: 45nm · 22nm · 14nm · 7nm

Latest analytical models with paper citations  |  For use in ngspice / MATLAB simulation

SECTION 1 — INTERCONNECT GEOMETRY PARAMETERS

All electrical parameters depend first on physical wire dimensions per technology node. The table below uses ITRS 2009 (for 45nm/22nm), ITRS 2.0 2015 (for 14nm), and IRDS 2022 (for 7nm) as sources for nominal dimensions.

| Parameter | 45nm | 22nm | 14nm | 7nm | Source |
| --- | --- | --- | --- | --- | --- |
| Wire Width W (nm) | 45 | 22 | 14 | 7 | ITRS 2009 / IRDS 2022 |
| Aspect Ratio (H/W) | 1.7 | 1.8 | 1.9 | 2.0 | ITRS 2009 |
| Wire Height H (nm) | 76.5 | 39.6 | 26.6 | 14 | Derived from AR |
| Wire Spacing S (nm) | 45 | 22 | 14 | 7 | ITRS (S = W assumed) |
| Dielectric constant k | 3.0 | 2.7 | 2.5 | 2.3 | ITRS 2015 / IRDS 2022 |
| Barrier thickness (nm) | 3.5 | 2.0 | 1.5 | 1.0 | ITRS 2009 |
| Effective Cu width (nm) | 38 | 18 | 11 | 5 | W - 2×barrier |
| Grain size D (nm) | 45 | 22 | 14 | 7 | D ≈ W (standard assumption) |
| CNT diameter d (nm) | 1.6 | 1.2 | 1.0 | 0.8 | Naeemi & Meindl 2007 |
| CNT bundle Fm | 0.33 | 0.33 | 0.33 | 0.33 | Unsorted synthesis (1/3) |

Note: For barrier layer, ITRS defines a TaN/Ta bi-layer. Effective Cu cross-section = (W - 2×t_barrier) × (H - t_barrier). At 7nm the barrier consumes ~29% of the width — include this in resistance calculations.

Sources: ITRS 2009 Interconnect Chapter; ITRS 2.0 (2015); IEEE IRDS More Moore 2022 [irds.ieee.org]

SECTION 2 — COPPER INTERCONNECT MODEL (Latest Formulas)

## 2.1  Resistance — FS + MS Combined Model

The most current and widely accepted resistivity model for scaled Cu interconnects combines Fuchs-Sondheimer (FS) for surface scattering and Mayadas-Shatzkes (MS) for grain boundary scattering. The latest form, validated experimentally below 14nm (AIP Advances 2019), uses the full integral FS expression rather than the approximate linear form used in older papers.

### Full FS Equation (surface scattering):

ρ_FS = ρ₀ × [1 - (3λ/2d)(1-p) ∫₁^∞ (1/t³ - 1/t⁵)(1 - e^(-kt))/(1 - p·e^(-kt)) dt]^(-1)

where:  k = d/λ,   d = min(W, H) = limiting dimension,   λ = 39 nm (Cu MFP at 21°C)

p = specularity parameter: 0.0 (fully diffuse) to 1.0 (specular)

Recommended value: p = -0.2 for sub-14nm nodes (AIP Advances 2019 experimental fit)

### Simplified FS Approximation (acceptable for 45nm/22nm nodes):

ρ_FS/ρ₀ = 1 + (3λ/8d)(1 - p)       [valid when d >> λ, breaks down below ~30nm]

### MS Equation (grain boundary scattering):

ρ_MS = ρ₀ × [1 - (3α/2) + 3α² - 3α³·ln(1 + 1/α)]^(-1)

α = (λ/D) × R/(1 - R)

where:  D = grain size ≈ wire width W (standard assumption),   R = GB reflection coeff. = 0.16–0.17 (AIP Advances 2019)

### Combined Effective Resistivity:

ρ_eff = ρ_FS × (ρ_MS / ρ₀)       [multiplicative combination — standard in literature]

R_cu = ρ_eff / (W_eff × H_eff)   [Ω/m, per unit length]

W_eff = W - 2×t_barrier,   H_eff = H - t_barrier   (accounts for non-conducting barrier layer)

Primary Reference [Cu-R1]: Smith, R.S., Ryan, E.T., Hu, C.-K. et al. 'An evaluation of Fuchs-Sondheimer and Mayadas-Shatzkes models below 14nm node wide lines.' AIP Advances, 9(2), 025015, 2019. DOI: 10.1063/1.5063896 [Corrected: earlier draft misattributed authors and DOI]

Secondary Reference [Cu-R2]: Camacho, J.M. & Oliva, A.I. 'Epitaxial metals for interconnects beyond Cu.' arXiv:2004.00971, 2020. [Provides FS integral + MS unified form]

Parameter Reference [Cu-R3]: Saligram, R. et al. 'Resistivity Modeling of Scaled Cu and Ru Interconnects.' IEEE TCAS-I, 2022. [Georgia Tech — validated at 7nm node]

| Node | ρ_bulk (μΩ·cm) | ρ_FS correction | ρ_MS correction | ρ_eff (μΩ·cm) approx |
| --- | --- | --- | --- | --- |
| 45nm | 1.68 | ~1.4× | ~1.3× | ~3.1 |
| 22nm | 1.68 | ~2.1× | ~1.8× | ~6.3 |
| 14nm | 1.68 | ~3.2× | ~2.4× | ~12.9 |
| 7nm | 1.68 | ~5.8× | ~3.9× | ~38.0 |

Note: The ~38 μΩ·cm at 7nm is over 22× the bulk value of 1.68 μΩ·cm — this is the key motivation for CNT replacement. Use these approximate multiplied values for a quick sanity check of your simulation output.

## 2.2  Capacitance — Sakurai-Tamaru Empirical Model

The Sakurai-Tamaru (1983) formula, updated with ITRS fringe-fitting coefficients, is the standard for Cu interconnect capacitance in VLSI papers. It captures both parallel-plate and fringe field contributions in a single closed-form expression.

### Total Capacitance Per Unit Length:

C = ε₀·εᵣ × [W/H + 2.04·(S/(S+0.54·H))^1.77 + 1.14·(W/H)^0.06·(S/(S+1.51·H))^4.53]

where:  ε₀ = 8.854×10⁻¹² F/m,   εᵣ = dielectric constant from table above,   S = wire spacing,   H = ILD height

CAUTION — unverified attribution: the original Sakurai-Tamaru (1983) formula for a single wire over a ground plane is C/ε = 1.15(W/H) + 2.80(T/H)^0.222 — a two-term expression with no spacing (S) dependence. The three-term formula above, with its specific exponents (1.77/0.06/4.53), does not match the 1983 paper. It is most likely the ITRS-fitted variant from Li et al. 2006 (APMC) referenced below — confirm the exact coefficients against that paper before citing this as "Sakurai-Tamaru 1983" in your report.

Reference [Cu-C]: Sakurai, T. & Tamaru, K. 'Simple formulas for two- and three-dimensional capacitances.' IEEE Trans. Electron Devices, 30(2), 183-185, 1983.

Updated coefficients: Li, H. et al. 'Modeling of Carbon Nanotube Interconnects and Comparative Analysis with Cu Interconnects.' APMC 2006 — uses this same Sakurai model with ITRS-fitted coefficients for 45nm node.

## 2.3  Inductance — Rectangular Wire Over Ground Plane

For Cu self-inductance, the Neumann formula for a rectangular cross-section wire is used:

L_self = (μ₀/2π) × [ln(2l/(W+H)) + 0.5 + 0.2235·(W+H)/l]   [H, total]

L_per_unit = L_self / l   [H/m]

where:  μ₀ = 4π×10⁻⁷ H/m,   l = wire length,   W = wire width,   H = wire height

For mutual inductance between adjacent parallel wires (needed for crosstalk):

M = (μ₀·l/2π) × [ln(2l/d) - 1 + d/l]

where:  d = center-to-center distance between wires = W + S

Reference [Cu-L]: Parihar, T. & Sharma, A. 'A comparative study of Mixed CNT bundle with Copper for VLSI Interconnect at 32nm.' IJETT, Vol.4(4), 2013. [Equations 6 & 7 — standard Neumann form]

SECTION 3 — SWCNT BUNDLE INTERCONNECT MODEL (Latest Formulas)

The CNT bundle model below is based on the latest physics-based formulation from MDPI Crystals 2022, which supersedes the earlier Naeemi & Meindl 2007 form by including temperature-dependent phonon scattering and improved contact resistance modeling. This version is directly citable in a 2024–2026 report. Note: this entire section applies to single-walled CNT (SWCNT) bundles only — the 4-conducting-channel convention, v_F, and phonon MFPs used throughout are SWCNT-specific. A multi-walled CNT (MWCNT) bundle would require a separate shell-resistance model and is not covered here.

## 3.1  Bundle Geometry

### Total CNTs in Bundle (hexagonal packing):

N_total = int(W/(d+δ)) × int(H/(d+δ))

where:  d = CNT diameter,   δ = 0.34 nm (van der Waals inter-tube spacing),   W×H = bundle cross-section

### Number of Metallic CNTs:

N_m = round(N_total × F_m),   F_m = 1/3  (unsorted synthesis)

For sorted/aligned synthesis: F_m can reach 1.0; cite the synthesis method used in your assumption.

## 3.2  Resistance (Latest Model with Phonon Scattering)

The 2022 MDPI model introduces an effective mean free path λ_eff that accounts for both acoustic (AC) and optical (OP) phonon scattering, making it more accurate at sub-22nm nodes than the fixed λ_mfp = 1μm assumption used in older papers.

### Effective Mean Free Path (temperature-dependent):

1/λ_eff = 1/λ_AC + 1/λ_OP

λ_AC = 400/(T/300) nm   [acoustic phonon MFP, T in Kelvin]

λ_OP = 56 nm            [optical phonon MFP, approximately temperature-independent]

At T = 300K:  λ_AC = 400 nm,  λ_OP = 56 nm  → λ_eff ≈ 48.8 nm

### Per-CNT Resistance (full model):

R_CNT = R_Q + R_scatter(L) + R_contact

R_Q = h/(4e²) ≈ 6.45 kΩ   [quantum/contact resistance per CNT, 4 channels]

R_scatter = (h/4e²) × (L/λ_eff)   [scattering resistance, length-dependent]

R_contact = R_C   [imperfect metal-CNT contact, 3.2–100 kΩ; cite your chosen value]

### Bundle Resistance Per Unit Length:

R_bundle = R_CNT / N_m   [parallel combination of metallic CNTs]

R_per_length = R_bundle / L   [Ω/m]

Note: R_contact value is the largest source of uncertainty. The MDPI 2022 paper uses 3.2 kΩ as a lower bound (best-case Pd contacts); many simulation papers use 10 kΩ as typical. State your assumption explicitly and perform a sensitivity analysis if time permits.

Primary Reference [CNT-R]: Majumder, M.K. et al. 'A Theoretical Modeling of Adaptive Mixed CNT Bundles for High-Speed VLSI Interconnect Design.' MDPI Crystals, 12(2), 186, 2022. DOI: 10.3390/cryst12020186

Phonon MFP Reference [CNT-R2]: Park, J.Y. et al. 'Electron-phonon scattering in metallic single-walled carbon nanotubes.' Nano Letters, 4(3), 517–520, 2004.

## 3.3  Inductance

Two inductance components contribute: kinetic inductance (dominant, quantum mechanical, due to electron inertia in 1D conduction channels) and magnetic inductance (classical, from geometry).

### Kinetic Inductance Per CNT (all 4 channels combined):

L_K_tube = h/(4e²·v_F) ≈ 8.07 nH/μm

where:  v_F = 8×10⁵ m/s (Fermi velocity in metallic SWCNT). Note: this uses 4e², the same whole-tube (4-channel) convention as R_Q = h/4e² above — it is NOT a per-single-channel value, so it must not be divided by an extra channel-count factor when computing the bundle total below.

### Total Bundle Kinetic Inductance Per Unit Length:

L_K_bundle = L_K_tube / N_m   [H/m]

where:  L_K_tube = h/(4e²·v_F) is already the per-tube value (the 4e² term accounts for all 4 conducting channels of one metallic SWCNT, consistent with the R_Q = h/4e² convention used above). N_m identical tubes in parallel combine like resistors, so no additional channel-count factor is applied here.

### Magnetic Inductance Per Unit Length (same form as Cu):

L_M = (μ₀/2π) × ln(2H/W + 1)   [H/m, approximate for bundle geometry]

### Total Bundle Inductance:

L_total = L_K_bundle + L_M   [H/m]

Note: At long interconnect lengths (L >> λ_eff), kinetic inductance dominates over magnetic inductance by 2–3 orders of magnitude. This is the reason CNT interconnects show higher inductance than Cu — not a disadvantage for delay but relevant for signal integrity analysis.

Reference [CNT-L]: Naeemi, A. & Meindl, J.D. 'Performance Modeling for Single- and Multiwall Carbon Nanotubes as Signal and Power Interconnects in Gigascale Systems.' IEEE Trans. Electron Devices, 55(10), 2574–2582, 2008.

## 3.4  Capacitance

Two capacitance components appear: quantum capacitance (from the density of states at the Fermi level, intrinsic to the 1D conductor) and electrostatic capacitance (geometric, same origin as Cu).

### Quantum Capacitance Per CNT Per Unit Length:

C_Q = 4e²/(h·v_F) ≈ 193.7 aF/μm   [per CNT, all 4 channels in parallel]

Corrected value: earlier drafts of this sheet listed 96.5 aF/μm, which is the 2e²/(h·v_F) single-channel result and is inconsistent with the 4e² (whole-tube, 4-channel) convention used for R_Q and L_K_tube above. Use 193.7 aF/μm to stay consistent throughout.

### Total Bundle Quantum Capacitance Per Unit Length:

C_Q_bundle = C_Q × N_m   [F/m, all metallic tubes in parallel]

### Electrostatic Capacitance Per Unit Length:

C_E = 2πε₀εᵣ / ln(2y/d)   [F/m, CNT bundle to ground plane]

where:  y = height of bundle center above ground plane,   d = bundle diameter (outermost dimension),   εᵣ = dielectric constant

### Total Bundle Capacitance (series combination per channel):

1/C_total = 1/C_Q_bundle + 1/C_E   [F/m]

Note: C_Q_bundle is usually much larger than C_E at these dimensions, so C_total ≈ C_E in most simulations. However, always compute both explicitly for sub-14nm nodes where C_Q becomes comparable.

Reference [CNT-C]: Srivastava, N. et al. 'Carbon Interconnects: Implications for Performance, Power Dissipation and Thermal Management.' IEEE CICC, 2005. [First full 3D capacitance treatment for SWCNT bundles]

Updated model [CNT-C2]: Majumder, M.K. et al. MDPI Crystals, 12(2), 186, 2022. [Equations 21–23 — quantum + electrostatic for bundle, with ITRS node-wise dimensions]

SECTION 4 — PROPAGATION DELAY & PERFORMANCE METRICS

## 4.1  Elmore Delay (Closed Form)

t_D = 0.69 × R_driver × C_load + 0.38 × R_line × C_line + 0.69 × R_driver × C_line + 0.69 × R_line × C_load

Correction: an earlier draft of this sheet had 0.38 on the R_driver·C_load term; that is the coefficient for the distributed self-term (R_line·C_line) only. The driver-to-load and driver-to-line terms both carry 0.69, per Rabaey/Weste-Harris — corrected above.

Simplified form for a uniform RC line with driver resistance R_driver and load C_load:

t_D ≈ 0.69·R_driver·C_load + 0.38·R·C·L²

where R, C are per-unit-length values and L is total wire length. Use this for quick comparison before running SPICE.

## 4.2  Power Delay Product (PDP)

PDP = P_dynamic × t_D = (α × C_load × V_DD² × f) × t_D   [J per switching event]

α = activity factor (0.5 for 50% switching),   f = operating frequency,   V_DD = supply voltage

## 4.3  Energy Delay Product (EDP)

EDP = PDP × t_D = P × t_D²   [J·s]

EDP is the standard figure of merit in the IJETT (Parihar 2013) paper you uploaded. Use it in your comparative plots — CNT bundles show lower EDP than Cu for long interconnects (>200μm at 22nm and below) due to lower capacitance, even when delay is comparable.

SECTION 5 — COMPLETE REFERENCE LIST FOR YOUR REPORT

### Copper Interconnect References

[Cu-R1]  Smith, R.S., Ryan, E.T., Hu, C.-K. et al. 'An evaluation of Fuchs-Sondheimer and Mayadas-Shatzkes models below 14nm node wide lines.' AIP Advances, 9(2), 025015, 2019. DOI: 10.1063/1.5063896

[Cu-R2]  Camacho, J.M. & Oliva, A.I. 'Epitaxial metals for interconnects beyond Cu.' arXiv:2004.00971, 2020. [Full FS integral + combined FS-MS model]

[Cu-R3]  Saligram, R. et al. 'Resistivity Modeling of Scaled Cu and Ru Interconnects for Advanced VLSI Nodes.' IEEE TCAS-I, 2022. DOI: 10.1109/TCAS1.2022.XXXXXX

[Cu-C]  Sakurai, T. & Tamaru, K. 'Simple formulas for two- and three-dimensional capacitances.' IEEE Trans. Electron Devices, 30(2), 183-185, 1983.

[Cu-L]  Parihar, T. & Sharma, A. 'A comparative study of Mixed CNT bundle with Copper for VLSI Interconnect at 32nm.' IJETT, 4(4), 2013. [Equations 6-7 for inductance]

### CNT Bundle References

[CNT-R1]  Majumder, M.K. et al. 'A Theoretical Modeling of Adaptive Mixed CNT Bundles for High-Speed VLSI Interconnect Design.' MDPI Crystals, 12(2), 186, 2022. DOI: 10.3390/cryst12020186  [PRIMARY — use for all CNT equations]

[CNT-R2]  Park, J.Y. et al. 'Electron-phonon scattering in metallic single-walled carbon nanotubes.' Nano Letters, 4(3), 517-520, 2004. [Phonon MFP values used in λ_eff formula]

[CNT-L]  Naeemi, A. & Meindl, J.D. 'Performance Modeling for Single- and Multiwall Carbon Nanotubes as Signal and Power Interconnects in Gigascale Systems.' IEEE Trans. Electron Devices, 55(10), 2574-2582, 2008.

[CNT-C]  Srivastava, N. et al. 'Carbon Interconnects: Implications for Performance, Power Dissipation and Thermal Management.' IEEE CICC, 2005.

### Technology Roadmap References

[ITRS-09]  International Technology Roadmap for Semiconductors (ITRS) 2009 Edition — Interconnect Chapter. Available: semiconductors.org/wp-content/uploads/2018/09/Interconnect.pdf

[ITRS-15]  International Technology Roadmap for Semiconductors 2.0 (ITRS 2.0) 2015 Edition — Interconnect Chapter.

[IRDS-22]  IEEE International Roadmap for Devices and Systems (IRDS) 2022 Edition — More Moore Chapter. Available: irds.ieee.org

### Comparative Study References

[CMP-01]  Naeemi, A. et al. 'Performance comparison between carbon nanotube and copper interconnects for GSI.' IEEE Electron Device Letters, 26(2), 84-86, 2005.

[CMP-02]  Li, H. et al. 'Modeling of Carbon Nanotube Interconnects and Comparative Analysis with Cu Interconnects.' Asia-Pacific Microwave Conf. (APMC), 2006.

[CMP-03]  Srivastava, N. & Banerjee, K. 'Performance analysis of carbon nanotube interconnects for VLSI applications.' IEEE/ACM ICCAD, 2005.

End of Formula Reference Sheet  |  VLSI Internship Project 2026  |  Assam University